## Slide 1
Development of high-performance room-temperature gas sensor using visible light activation of photosensitizer
GIST SMSE- NTUST SYMPOSIUM
Presenter : Yeonji Yuk
Advisor: Sanghan Lee
Sustainable Energy and Electronic Devices Lab. (SEED)
School of Materials Science and Engineering (SMSE)
Gwangju Institute of Science and Technology (GIST)
2024.10.17

## Slide 2
Rising demand for gas sensors in various industries
Ref) Mater. Horiz., 2021, 8, 661
Ref) frontiersin.org
The demand for gas sensors is increasing.
Electrode
Heater
Substrate
Insulator
Sensing material
(metal oxide)
Drawback
Operating temperature > 473.15K
Heater required
It is crucial to develop Room temperature(RT) gas sensors.
Notes: There are a lot of various gases in our environment.
The detection of toxic, harmful and volatile gases cannot be separated form gas sensor.
It is used to monitor food spoilage, health care and air pollution.
So, the demand is increasing.
Chemiresistive type gas sensor uses mostly metal oxide as sensing layer because of cost and stability.
However, operating high temperature is essential to enhance the sensitivity of gas sensor, so heater must be required.
It cause high power consumption and poor device lifetime, so it’s important to develop room temperature gas sensors.

## Slide 3
Issue
Visible light-activated room-temperature gas sensors using metal oxide
Ref) Small Struct. 2024, 5, 2300503
Ref) Adv. Mater. 2024, 36, 2313731
Metal halide perovskite(MHP) Photosensitizer
1) Light source : UV LED
Advantages
Tunable narrow bandgap
Excellent photoactive properties
Facile synthesis
Disadvantages
Degradation in the humidity environment >> solved by encapsulation engineering
High power consumption, Harmful to human health
2) Rampant use of Noble metal
High cost, Scarcity
Ref) Small Methods, 2024, 8, 2300417
“Visible light”
Ref) Adv. Funct. Mater. 2024, 34, 2312175
“Suitable to
photosensitizer material”
3/11
Encapsulation Engineering
Notes: Light activation have attracted attention as alternative energy to heater.
Many researcher has studied the decoration of metal oxide surface with noble metal under ultraviolet.
But UV requires high power consumption and is harmful to human health. Also, noble metal has cost issue.
Therefore, we need to find new non noble metal material that can be operate under long wave lengths.
we focused on perovskite material as non noble metal photosensitizer under visible light.
It has advantage of tunable narrow bandgap , excellent photoactive properties and easy synthesis.
Encapsulation engineering is an effective strategy to prevent perovskite degradation in humid environments.

## Slide 4
Fabrication of metal oxide-based RT gas sensor using MHP
Strategy 1. porous nanostructure
Strategy 2. photosensitizer decoration: MHP
Target gas
Visible
Light
CsPbBr3@ SiO2
Increase electron density under green light
Inorganic halide perovskite
Stable humidity condition
Tin dioxide(SnO2)
Well-aligned porous nanostructure
Dual valency with Sn oxidation state
via glancing angle deposition(GLAD)
4/11
Notes: Based on previous slide, the strategies is established as follow.
The first strategy is to maximizing surface area via glaning angle deposition. It can be fabricated well aligned porous nanostructure.
And we selected SnO2 which is easily adsorbed by oxygen due to dual valency with Sn oxidation state.
The second strategy is to decoreated MHP as photosensitzer.
It increase electron density under green light due to narrow bandgap and electron-hole pair generation.
Also, cesium lead bromide is consisted of inorganic halide material. It is more stable than other MHP.
And encapsulating SiO2 shell also improves stability under humidity condition.

## Slide 5
Material process
Axis Rotation
Angle control
Pt 50nm /Ti 3nm
SiO2 100nm/ Si
Crucible(SnO2)
SnO2
CsPbBr3
Heating zone
sample
holder
873.15K, 2hour, air
CsPbBr3
NC
3. Colloidal synthesis
4. Spin coating
5. Drying
GLAD
2. Post annealing
Collaborated with
Dr. Chang-Lyoul Lee(APRI)
Light 505nm
Gas
In
5/11
Notes: we synthesized and analysis the sensing layer using the following process.

## Slide 6
morphology characterization
The SEM images show that vertically aligned 100 nm SnO2 nanorods array was deposited via GLAD.
TEM image reveals that 13 nm SiO2@CsPbBr3 nanocubes array were synthesized via colloidal method.
SiO2@CsPbBr3 nanocubes was decorated on SnO2 nanorod without collapse of the structure.
Scanning Electron Microscopy (SEM) cross image
Transmission Electron Microscopy
(TEM) image
SEM tilt image
100nm
CsPbBr3 @ SiO2 nanocubes/SnO2 nanorod
6/11
Notes: TEM and SEM images confirmed the successful synthesis of Vertically align SnO2 nanorod array and CsPbBr3 encapsulated in SiO2.
Also, right image reveals that Photosensitizer is decorated on SnO2 nanorod without collapse of the structure.

## Slide 7
Crystallinity & optical characterization
Photoluminescence (PL)
X-ray Diffraction (XRD)
PL peak:
513 nm
XRD data reveals SnO2 rutile phase and CsPbBr3@SiO2 cubic phase are observable without any phase change.
PL data shows that CsPbBr3@SiO2 /SnO2 wavelength is same as CsPbBr3@SiO2 .
The bandgap decorated with CsPbBr3@SiO2 was found to be approximately 2.41 eV and 2.44 eV, which is a red shift from pristine SnO2 (Eg=2.67 eV).
Tauc plot
~2.44 eV
~2.67 eV
~2.41 eV
7/11
PL intensity (a.u)
Wavelength (nm)
Photon energy (eV)
()2
Intensity (a.u)
2 ()
Notes: When PQD decorated on SnO2, it show same crystallinity and optical property compared to pristine.
it demonstrate that the phase or wavelength has not change.
And the band gap is red shift from pristine tin oxide, it reveal that it can be possible to absorbed green light.

## Slide 8
Gas sensing properties
CsPbBr3@SiO2/SnO2 NR under dark and Light 505nm
CsPbBr3@SiO2/SnO2 shows n-type oxide semiconductor gas sensor mechanism.
The presence of CsPbBr3@SiO2 doesn’t affect response and recovery time under dark.
Sensitivity and response/recovery time is improved under light 505nm.
2.09
269s
-s
8/11
Response (Ra/Rg)
116s
129s
19.45
Response (Ra/Rg)
Time (min.)
Time (min.)
Notes: And then, we analysis gas sensing property under dark and 505nm wavelength as green light.
Both are shown n-type oxide semiconductor mechanism.
The presence of SiO2@CsPbBr3 doesn’t affect response and recovery time under dark.
On the other hand, when green light source is irradiated, sensitivity and recovery/response time is improved.

## Slide 9
Gas sensing properties
Selectivity test
Long stability test
Reproducibility test
When compared to other reference gases, SiO2@CsPbBr3/SnO2 shows excellent NO2 Selectivity.
it exhibited stable performance over 3 cycle and 3 days through reproducibility and long stability test.
9/11
Gas in
Gas out
Day1
Day2
Day3
13.8-fold
Response (Ra/Rg)
Response (Ra/Rg)
Response (Ra/Rg)
Time (min.)
NO2
NH3
H2S
CO
H2
Acetone
Analytes
Notes: It shows excellent NO2 selectivity compared to other reference gases.
Finally, it exhibit stable performance 3 cycle and 3 days through reproducibility and long stability test.

## Slide 10
Suggested gas sensing mechanism
Time Resolved Photoluminescence(TRPL)
Sample condition | 1 [ns] (f1) | 2 [ns] (f2) | 3 [ns] (f3) | ave [ns]
CsPbBr3@SiO2/SnO2 before | 0.356 (0.66) | 6.703 (0.02) | 1.615 (0.32) | 0.921
CsPbBr3@SiO2/SnO2 NO2 exposed | 0.615 (0.50) | 7.447 (0.07) | 2.194 (0.43) | 1.769
CsPbBr3@SiO2/SnO2 after recovery | 0.329 (0.58) | 7.581 (0.05) | 1.744 (0.37) | 1.183
Sample condition |  |  |  | 
CsPbBr3@SiO2/SnO2 before | 0.356 (0.66) | 6.703 (0.02) | 1.615 (0.32) | 0.921
CsPbBr3@SiO2/SnO2 NO2 exposed | 0.615 (0.50) | 7.447 (0.07) | 2.194 (0.43) | 1.769
CsPbBr3@SiO2/SnO2 after recovery | 0.329 (0.58) | 7.581 (0.05) | 1.744 (0.37) | 1.183
Photoluminescence(PL)
PL data indicates that electrons have transferred from CsPbBr3 to SnO2 .
TRPL data shows distinct trend in 3 which is longer decay time when NO2 exposed.
10/11
CsPbBr3@SiO2/SnO2 : ~21% decrease
CsPbBr3@SiO2 : ~1% decrease
Integrated PL int. (x106 cnt.)
NO2 exposed
Notes: To prove the role of the photosensitizer, we analyzed the mechanism via PL and TRPL.
PL intensity decrease after exposure to NO2 gas compared to pristine perovskite. It indicates that electron have transferred from CsPbBr3 to SnO2.
Furthermore, TRPL data revealed distinct trend in tau 3 which is longer decay time when NO2 exposed.

## Slide 11
SiO2@CsPbBr3/SnO2
It can be operated at room temperature under green light.
It exhibited significantly fast recovery and high response compared to pristine SnO2.
The photosensitizer mechanism is demonstrated via PL intensity and TRPL.
11/11
116s
129s
19.45
Response (Ra/Rg)
Light
source
Gas
In
Probe Tip
<Light>
Notes: It can be operated at room temperature undere green light and exhibited fast recovery and high response compare to pristine SnO2.
Also the phososensitizer mechanism is demonstrate via PL intensity and TRPL.

## Slide 14
Ref) Sensors and Actuators B 169 (2012) 199–207

## Slide 15
SiO2 shell
SiO2@CsPbBr3

## Slide 16
Pristine SnO2 NR
Response : 1.74
Response time : 269s
Recovery time: -s
Response : 2.86
Response time : 273s
Recovery time: -s
Pristine SnO2 is shown n-type oxide semiconductor gas sensor mechanism.
Photoactivation affects the recovery time of pristine SnO2 due to reactive oxygen species and electron-hole pair.
5.0E+04
3.4E+04
2.9E+02
Response : 5.73
Response time : 40s
Recovery time: 455s

## Slide 17
CsPbBr3/SnO2 NR
Test 1)
Response time : 55s
Recovery time: 265s
Test 2) Response time : 54s
Recovery time: 260s
With each cycle, there is a decrease in response due to CsPbBr3 core only photosensitizer degradation.
Response | test1 | test2
1cycle | 7.82 | 7.82
2 cycle | 5.16 | 4.73
3 cycle | 2.81 | 3.94

## Slide 18
SiO2@CsPbBr3: ~2.9% decrease
CsPbBr3 : ~59% decrease
CsPbBr3 film PL intensity
CsPbBr3 /SnO2 film
SiO2@CsPbBr3 /SnO2: ~27.6% decrease
CsPbBr3 /SnO2 : ~22.4% decrease

## Slide 19
TRPL

## Slide 20
TRPL
Sample condition | τ1 [ns] (f1) | τ2 [ns] (f2) | χ2 | τave [ns]
SiO2@CsPbBr3 before | 0.696 (0.78) | 2.937 (0.22) | 1.171 | 1.189
SiO2@CsPbBr3 after | 0.724 (0.76) | 2.908 (0.24) | 1.169 | 1.252
CsPbBr3 before | 0.998 (0.73) | 3.909 (0.27) | 1.209 | 1.781
CsPbBr3 after | 1.059 (0.69) | 4.194 (0.31) | 1.264 | 2.036
=0.028ns
=0.061ns
<