## Slide 1
Global Photovoltaic Conference 2023
Advanced Photoelectrochemical Ammonia Production via Tailoring Catalyst-Electrolyte Microenvironment
Yejoon Kim, and Sanghan Lee*
School of Materials Science and Engineering, Gwangju Institute of Science and Technology (GIST), Gwangju, Korea
E-mail: ssh8455@gm.gist.ac.kr, sanghan@gist.ac.kr
1. Introduction
Ammonia (NH3) is a valuable chemical in a variety of applications, including fuel cells, fertilizers, and hydrogen carriers. Photoelectrochemical (PEC) conversion of N2 to NH3 is a sustainable alternative to the Haber-Bosch process, which emits significant greenhouse gases. However, its practical application has been challenged by low production yields due to low N2 adsorption selectivity.
Tailoring catalyst-electrolyte microenvironments is a promising strategy to improve the performance and practicality of photoelectrochemical NH3 production. We tried to control the microenvironment near the MoS2 catalyst surface via cation and anion exchange ionomers. (Nafion & Sustainion)
Our results show that the use of these ionomers induced a significant increase in NH3 yields and conversion efficiency, suggesting that a tailored catalyst-electrolyte microenvironment maximized the N2 adsorption selectivity of the catalyst layer, thereby improving the performance of photoelectrochemical NH3 production.
Schematic of a study
Mechanism of NRR [1]
2. Experimental methods
Pulsed laser deposition
Ionomer coating
Using the pulsed laser deposition method (PLD) method, we fabricated the edge-exposed MoS2 catalyst layer on a centimeter scale.
The edge-exposed MoS2 has been reported to be electrocatalytically active sites for N2 reduction (by DFT calculations).[2]
The ionomer layers were coated on the catalysts by drop casting method.
3. Results
SEM images
Edge-exposed MoS2 was uniformly deposited on the pyramid Si-photocathode.
Raman spectrum
PEC activity of MoS2
Coated ionomers
Edge-exposed MoS2/Si photocathodes show high PEC activity for HER.
Nafion coating
Sustainion coating
Both the nafion and the sustainion ionomers were coated without damaging the MoS2 catalyst layer.
They are transparent and do not interfere with the light absorption of the photoelectrode.
Nafion
Sustainion
Production yield
by Nafion concentration
by Sustainion concentration
Ionomer bilayer (Naf/Sus)
Cycling test
The 0.03 wt.% of sustainion worked best among the ionomer monolayers.
When 0.04 wt.% of nafion was added on top of it, the effect was even higher.
Over the cycling test, it produced NH3 at a high FE% while maintaining a current density of over 3 mA cm-2.
4. Conclusion
Using a pulsed laser deposition method, we fabricated an edge-exposed MoS2 catalyst layer with potentials for NRR.
Using an ionomer bilayer, we optimized the microenvironment of the MoS2 catalyst for NRR by suppressing HER and enriching nitrogen-containing TPCPs.
It showed an excellent ammonia yield of 145.83 μg h-1 cm-2 and an efficiency of 23.7 %.
5. References
[1] Chen, X. et al. Adv. Energy Mater. 2020, 10, 1903172.
[2] Zhang, L. et al, Adv. Mater. 2018, 30, 1800191.