## Slide 1
Photoelectrochemical Glycerol Selective Oxidation of Oxygen Vacancy Modulated WO3
Yoonsung Jung, Sanghan Lee∗
School of Materials Science and Engineering, Gwangju Institute of Science and Technology (GIST), Gwangju, 61005, Korea

## Slide 2
Needs of Renewable Energy Source
Use of Renewable Energy Source
Reduction of Greenhouse Gases
Production of Valuable Energy Source
Issues
Paris Climate Agreement
Green new deal
hv
Solar
Electrolyte
Electrode
Photoelectrochemical system
+
Valubable Energy Source

## Slide 3
What is the glycerol
Biofuel
Source: European Biofuel Portal
Byproduct
Glycerol
Byproduct of biodiesel
High viscosity
Low value
Pharamaceutical
Cosmetic
Medicine
Chemical
Fuel
Valuable products
Needs to be conberted to

## Slide 4
Principles of Photoelectrochemical Glycerol Oxidation
vs. PEC Water Oxidation
vs. PEC Glycerol Oxidation
Slow reaction
Oxidation: 2H2O + hv → O2 + 4H+ + 4e-
Fast reaction compared Water Oxidation
Oxidation: C3H8O3 + hv → C3H6O4, C2H4O3, CH2O2, and etc…
Photon-generated hole easily oxidizes glycerol
Glycerol oxidation requires much less energy than water oxidation

## Slide 5
Photoelectrochemical glycerol selective oxidation
Applied Catalysis B: Environmental, 106(1-2), 123-132.
Chemical Structure
Glycerol oxidation path
Chemical structure with three hydroxyl groups
More thermodynamically stable of low value-added products

## Slide 6
Photoelectrode
Tugsten oxide (WO3)
Glycerol oxidation system still need consideration
W
O
Catalysis Today, 352, 73-79.
Small, 13(31), 1701354.
Acid sites and vacancies influence C-OH oxidation
Glycerol selective oxidation by oxygen vacancy modulated
Glycerol
(GLY)
Glyceraldehyde
(GLA)

## Slide 7
Experimental Setup
Solvothermal synthesis
Substrate
Solution
Autoclave set
Hydrothermal
synthesis
Annealing
160 °C
500 °C
WO3 synthesis
Argon/oxygen
blend
Oxygen

## Slide 8
Results and Discussion
Raman spectra
𝒗(o-w-o)
δ (o-w-o)
𝒗(W2O6 & W3O8)
𝒗a(o-w-o)
WO3(H2O)0.333
FTO
XRD
Annealing
WO3
WO3 were successfully synthesized
Vacancy modulated have no noticeable effect on WO3 structure

## Slide 9
Results and Discussion
WO3 (bare)
WO3 (O/Ar)
Ov:OL = 1 : 2.2
OV:OL = 1 : 3.0
<
XPS
rich vacancy
poor vacancy
FTIR
L
B&L
B
B
WO3 (O/Ar) has a larger area of Ov (oxygen vacancy orbital) than WO3 (bare)
Oxygen vacancies contributes to the formation of Lewis acid sites and Bronsted acid sites.
Bare (CL : CB = 1 : 1.1)
O/Ar (CL : CB = 1: 1.2)
Bare (CL+ CB) < O/Ar (CL+ CB)

## Slide 10
Results and Discussion
Photoelectrochemical performance
WO3 (bare)
WO3 (O/Ar)
Electrolyte : 0.5 M Na2SO4 with/without 2 M glycerol, the pH value was adjusted to 2 by H2SO4
Charge separation efficiency improved by vacancy-modulate

## Slide 11
Results and Discussion
Photoelectrochemical performance
WO3 (bare)
WO3 (O/Ar)
Extract
Extract
Extract
Extract
Extract
Extract
Stable photoelectrochemical reaction for 5 hours
For each potential, samples were collected at 1 h, 3 h, and 5 h of reaction

## Slide 12
Results and Discussion
GLA
Quantification analysis (HPLC)
Glycerol can be selectively converted to glyceraldehyde by oxygen vacancy modulated WO3

## Slide 13
Summary
WO3 on FTO coated glass substrates was successfully fabricated using a solvothermal technique
Oxygen vacancy concentration modulated by annealing condition
The most formed products of glycerol oxidation are glyceraldehyde
Glyceraldehyde accounts for an overwhelming production and it has significant ratio due to the possession of electrode's selectivity

## Slide 14
Thank you for your attention!